GRADE-SECTION PRODUCTS ASSORTMENT 

of the JSC „Zlatoust

Metallurgical Plant“ 

EXPORT

Contents

1. STEEL GRADES AND STANDARDS FOR THE DELIVERY

1.1.Constructional steel grades:

-general use(
-carbon steels(
-manganese steels(
-carburizing and nitriding steels(
-heat treatable steels.

APPENDIXES:

-steelmaking(
-hardness in delivery state.

1.2. Corrosion-resistant steel grades:

-martensitic-ferritic and martensitic steel grades(
-austenitic steel grades.

1.3.Tool steel grades

     (including high-speed)

2. SHAPES, DIMENSIONS, CROSS-SECTIONS, SHAPES AND DIMENSIONS DEVIATIONS

3.SURFACE QUALITY REQUIREMENTS

1.1.CONSRUCTIONAL STEEL GRADES

of ordinary quality, general use

STEEL GRADES AND STANDARDS FOR THE DELIVERY

	DIN 17100
	ASTM A-29

ANALOGUE
	GOST 380-94

	St37.2(1.0037)
	1015
	Ст3сп

	44.2
	~1023
	Ст4сп

	52.3
	~1030
	Ст5сп

	60.2
	~1042
	Ст6сп


KIND OF PRODUCTS

Bloom with cross-section of 170-250mm and square steel billet of 50-160mm (with /without heat treatment)

Bars of  diameter:

- 14-190mm with surface peeling (with/without heat treatment);

-15-150mm without surface peeling (with/without heat treatment);

-bars with special surface finishing, dia. 2-120mm (ground, polished, with/without heat treatment)

-square steel billet, cross section of  50-120mm, suitable for the following heat treatment , including upsetting, forging, hot forming with/without heat treatment.

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure

-ultrasonic test

-mechanical properties

-grain size

-hardenability

-hardness

-non-mixed test

CARBON CONSRUCTIONAL STEEL

                                  STEEL GRADES AND STANDARDS FOR THE DELIVERY
     GERMANY                       USA                  FRANCE               ITALY                                                RUSSIA

	DIN 17200
	ASTM

A-29
	AFNOR
	UNI
	EN 10083
	GOST 1050-88

analogue

	DIN 17210
	
	
	
	
	

	C15 (1.0401)
	1015
	XC12
	
	
	15

	CK15 (1.1141)
	1018
	XC18
	
	
	

	C22 (1.0402)
	
	
	
	1C22
	

	CK22 (1.1151)
	1020
	
	C20
	2C22
	20

	C25 (1.0402)
	
	
	
	1C25
	

	CK25 (1.1158)
	1025
	XC25
	C25
	2C25
	25

	C30 (1.0528)
	
	
	
	1C30
	

	CK30 (1.1178)
	1030
	XC32
	C30
	2C30
	30

	C35 (1.0501)
	
	
	
	1C35
	

	CK35 (1.1181)
	1035
	XC38
	C35
	2C35
	35

	C40 (1.0511)
	
	
	
	1C40
	

	CK40 (1.1186)
	1040
	XC42
	C40
	2C40
	40

	C45 (1.0503)
	
	
	
	1C45
	

	CK45 (1.1191)
	1045
	XC48
	C45
	2C45
	45

	C50 (1.0540)
	
	
	
	1C50
	

	CK55 (1.1206)
	1050
	
	C50
	2C50
	50

	C55 (1.0535)
	
	
	
	1C55
	

	CK55 (1.1203)
	1055
	XC55
	C55
	2C55
	55

	C60 (1.0601)
	
	
	
	1C60
	

	CK60 (1.1221)
	1060
	
	C60
	2C60
	60


KIND OF PRODUCTS

Bloom with cross-section of 170-250mm and square steel billet of 50-160mm (with /without heat treatment);

Bars of  diameter:

- 14-190mm with surface peeling (with/without heat treatment);

-15-150mm without surface peeling (with/without heat treatment);

-bars with special surface finishing, dia. 2-120mm (ground, polished, with/without heat treatment);

-square steel billet, cross section of  50-120mm, suitable for the following heat treatment , including upsetting, forging, hot forming with/without heat treatment.

NOTE: 

· the bars with dia. 14-190 mm are to be produced with Ca, N, or S micro-alloying to improve the mechanical treatment;

· the limited quantity of bars could be delivered in the normalized condition of the length up to 8,5 m
CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure

-ultrasonic test as per SEP 1921, class C/c

-mechanical properties on the heat treated samples or in the delivery condition

-non-metallic inclusions as per DIN 50602 (K4) or ASTM E45, (method A)

-grain size as per ASTM E112 or DIN 50601

-hardenability

-non-mixed test

-hardness
MANGANESE STEEL GRADES FOR THE MANUFACTURE OF FLANGES AND FITTING

                                  STEEL GRADES AND STANDARDS FOR THE DELIVERY

	ASTM
	GOST

	A-615
	4543-71
	5781-82
	19281-89

	A105
	20Г
	35ГС
	17ГС

	
	25Г
	25Г2С
	

	
	35Г
	
	

	
	40Г
	
	

	
	30Г2
	
	


KIND OF PRODUCTS

Bloom with cross-section of 170-250mm and square steel billet of 50-160mm (with /without heat treatment)

Bars of  diameter:

- 14-190mm with surface peeling (with/without heat treatment);

-15-150mm without surface peeling (with/without heat treatment);

-bars with special surface finishing, dia. 2-120mm (ground, polished, with/without heat treatment).

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure;

-mechanical properties: with/without control on the heat treated samples, or in the delivery condition.

CONSTRUCTIONAL ALLOY HEAT TREATABLE STEEL GRADES

STEEL GRADES AND STANDARDS FOR DELIVERY

     GERMANY                     USA                     FRANCE               ITALY                                                RUSSIA

	DIN 17200


	ASTM

A-29
	AFNOR


	UNI 


	EN 10083
	GOST 
analogue

	25CrMo4 (1.7218)
	4130
	25CD4
	25CrMo4
	25CrMo4
	25ХГМ

	42CrMo4 (1.7225)
	4140

4142
	42CD4
	42CrMo4
	42CrMo4

42CrMoS4
	38ХГМ

	30CrNiMo8

(1.6580)
	
	30CND8
	
	30CrNiMo8
	30X2H2M

	and other
	4135
	30CD4
	30CrMo4
	
	20ХН2М

	
	
	35NCD16
	
	
	30-35Х2Н4МА

	
	
	
	39NiCrMo3
	
	35ХНМ-40ХГНМ


KIND OF PRODUCTS

Bloom of cross-section of 170-250mm and square steel billet of 50-160mm (with /without heat treatment);

Bars of  diameter:

- 14-190mm with surface peeling (with/without heat treatment);

-15-150mm without surface peeling (with/without heat treatment);

-bars with special surface finishing, dia. 2-120mm (ground, polished, with/without heat treatment);

-square steel billet, cross section of  50-120mm, suitable for the following heat treatment, including upsetting, forging, hot forming with/or without heat treatment.

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure;

-ultra sonic test as per SEP 1921, class C/c;

-mechanical properties on the heat treated samples or in the delivery condition;

-non-metallic inclusions as per DIN 50602 (K4) or ASTM E45, method A (A,B,C,D);

-grain size as per ASTM E112 or DIN 50601;

-hardenability;

-non-mixed test;

-hardness;

CONSTRUCTIONAL CARBURIZING AND NITRIDING STEEL GRADES

STEEL GRADES AND STANDARDS FOR THE DELIVERY

               GERMANY                    FRANCE                     ITALY                            USA                         RUSSIAN

	DIN 17210
	AFNOR


	UNI
	ASTM

A-29
	GOST

analogue

	16MnCr5  (1.7131)
	16MC5
	16MnCr5
	
	18ХГ

	20MnCr5  (1.7147)
	20MC5
	20MnCr5
	
	18ХГ

	15CrNi6   (1.5919)
	16NC6
	
	
	14ХГН

	17CrNiMo6  (16587)
	30CD4

18CD6
	30CrMo4
	4135
	20ХН2М

	16CrMo4 (1.7242)
	
	18CrMo4
	
	20ХМ

	
	
	18NiCrMo5
	
	20ХГН2М

	21NiCrMo2  (1.6523)
	
	
	SAE 8620
	20ХГНМ

	15CrMoV5.9  (1.8521)
	
	
	
	25Х1МФА


KIND OF PRODUCTS:

Bloom of cross-section of 170-250mm and square steel billet of 50-160mm (with/without heat treatment);

Bars in a diameter:

-14-190mm with surface peeling (with/without heat treatment);

-15-150mm without surface peeling (with/without heat treatment);

-bars with special surface finishing, dia.2,0-120mm (ground, polished, with/without heat treatment);

-square steel billet suitable for the following heat treatment including upsetting/forging/hot forming with/without heat treatment.

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure;

-ultrasonic test as per SEP 1921, class C/c;

-mechanical properties on the heat treated samples or in the delivery condition;

-non-metallic inclusions as per DIN 50602 (K4) or ASTM E45, method A (A, B, C, D);

-grain size as per ASTM E112 or DIN 50601 (K4);

-hardenability;

-hardness;

-non-mixed test,.

APPENDIXES

CONSTRUCTIONAL STEEL GRADES
(STEELMAKING)

	ELECTRIC STEEL

	STEEL GRADE
	OPEN-HEARTH SHOP
	Open electric arc remelting
	With/without vacuum degassing

with/without

ladle furnace
	Vacuum arc remelting

Electro-slag remelting

induction furnace

	C20-C60
	+
	+
	+
	+

	16MnCr5,

20MnCr5
	+
	+
	+
	-

	St 52.3
	+
	+
	-
	-

	25Г,25Г2С
	+
	+
	-
	-

	35Г, 35С
	+
	+
	+
	-

	40Г
	+
	+
	-
	-

	CТ3СП-6СП
	+
	-
	-
	-

	St.37.2
	+
	+
	-
	-

	SAE 8620
	-
	+
	+
	+

	SAE 1055
	+
	+
	+
	+

	18CrMo4
	+
	+
	+
	+

	30CrMo4
	+
	+
	+
	+

	42CrMo4
	+
	+
	+
	+

	17CrNiMo6
	+
	+
	+
	+

	18CrNiMo5
	+
	+
	+
	+

	15CrMoV5.9
	-
	+
	+
	+

	30CrNoMo8
	-
	+
	+
	+

	39NiCrMo3
	+
	+
	+
	+

	35NCD16
	-
	+
	+
	+


Note: S, N, Ca -microalloyed steel should be melted only in the open arc furnaces

STEEL HARDNESS AS RECEIVED

provided with working technology.

	Steel grade
	Hardness in the delivery condition (max)

	CK15
	197

	CK15
	150

	ХС18
	156

	CK30
	180

	XC38
	183

	C45
	240

	CK45
	241

	CK45
	230

	XC48
	245

	16MnCr5(S)
	210

	16MC5
	225

	18CrMo4
	220

	20MnCr5
	255

	25CrMo4
	212


Note: for hardness guaranteeing bars may be subject to annealing

1.2. CORROSION-RESISTANT STEEL GRADES

MARTENSITIC-FERRITIC AND MARTENSITIC STEEL GRADES

STEEL GRADES AND STANDARDS FOR THE DELIVERY

	DIN 17440
	ASTM A-276, A-479
	GOST 5632-72 analogue

	X10Cr13  (1.4006)
	410
	12X13

	X20Cr13  (1.4021)
	420
	20X13

	X30Cr13  (1.4028)
	420F
	30X13

	X20CrNi17.2  (1.4057)

X17CrNi16.2
	431
	20X17H2


KIND OF PRODUCTS:

Bloom of cross-section of 170-250mm and square steel billet of 50-160mm 

(with heat treatment);

Bars in diameter:

-bars of 14-190mm with surface peeling (heat treatable or annealed);

-bars with special surface finishing dia.2,0-120mm as ground, polished (annealed).

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure

-ultrasonic test as per SEP 1921, class C/c

-mechanical properties in the delivery condition

-hardness, strength in the annealed condition

-hardness on the samples after upsetting (as required)

-impact test (as required)

AUSTENITIC STEEL GRADES

STEEL GRADES AND STANDARDS FOR THE DELIVERY

	DIN17440
	ASTM A-182, A-276, A-479
	GOST 5632-72

analogue

	X5CrNi18-10  (1.4301)
	304
	08X18H10

	X6CrNiTi 18-10  (1.4541)
	321
	08-12X18H10T

0612X18H10T

	X5CrNiMo 17-12-2  (1.4401)
	316
	06X17H13M2

	X6CrNiMoTi 17-12-2  (1.4571)
	316Ti
	10X17H13M2

	X2CrNi 19-11 (1.4306)
	304L
	03X18H11T


KIND OF PRODUCTS:

Bloom of cross-section of 170-250mm and square steel billet of 50-160mm (without heat treatment);

Bars in diameter:

-bars of 14-190mm with surface peeling; 

-bars with special surface finishing dia.2,0-120mm as ground, polished. 

CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure

-ultrasonic test as per SEP 1921, class C/c

-mechanical properties in the delivery condition

-non-metallic inclusions as per DIN 50602 (K4) or ASTM E45 method A (A, B, C, D)

-intergranular corrosion resistance 

1.3. TOOL AND HIGH-SPEED STEEL GRADES

STEEL GRADES AND STANDARDS FOR THE DELIVERY

	DIN 17350
	ASTM A-600, A-681
	GOST analogue

5950-2000, 19265-73

	X210CrW12  (1.2436)
	
	X12BM

	X210Cr12  (1.2080)
	D3
	X12

	X155CrVMo12-1  (1.2379)
	D2
	X12MФ

	90MnCrV8  (1.2842)
	02
	9Г2Ф

	X38CrMoV5.1 (1.2343)
	H11
	4X5МФС

	S 6-5-2  (1.3343)
	М2
	Р6М5

	S 6-5-2-5  (1.3243)
	
	Р6М5К5

	100MnCrW4  (1.2510)
	01
	9ХВГ

	56NiCrMoV7  (1.2714)
	L6
	5XHM


KIND OF PRODUCTS:

-round peeled bars of dia.14-150mm

-bars with special surface finishing dia.2,0-120mm as ground, polished (annealed)

-bars of a dia.15-105 mm, hot rolled, peeled, ground:  1.2436, 1.2080, 1.2379 (annealed);

-bars of a dia. 15-150 mm hot rolled, peeled, ground: 1.2842, 1.2343 (annealed);
-bars of a dia. 10-60mm as ground, polished: 1.3343, 1.3243 (annealed)
CHARACTERISTICS TO BE CONTROLLED (to be agreed when order is received):

-macrostructure

-ultra sonic test as per SEP 1921

-hardness

-decarburizing layer

-carbide inhomogeneity  as per DIN 17350 (sep 1615) or ASTM A-651

-non-metallic inclusions (except of high-speed steels) as per DIN 50602 (K4) or ASTM E45 method A (A, B, C, D)

2.SHAPES, DIMENSIONS, CROSS-SECTIONS, TOLERANCES FOR SHAPES AND DIMENSIONS

	Kind of products
	Dimension, mm
	Length, m

	bloom
	170-250
	3-5

	Square billet
	50-100
	4-6

	
	120
	5

	
	140-160
	2-3,5

	Round peeled bars
	14-80
	3-6

	
	> 80-190
	3-6

	Round bars without peeling
	15-150
	4-6

	Round bars with special surface finishing
	2-6
	1,5-2,5

	
	> 6-10
	1,5-3,5

	
	> 10-18
	2-4

	
	>18-120
	2,7-6


	Kinds of products
	Dimensions, mm
	Max. tolerances, mm


	Straightness

mm/1m

max
	Cutting oblique, mm, max
	Ovality,

%
	Twisting

Grad/m
	Diagonal difference

	Bloom
	170-180
	+/-5,0
	12
	20
	
	3
	0,7 of max side tolerances

	
	190-200
	+/-6,0
	12
	20
	
	3
	

	
	220-250
	+/-7,0
	12
	20
	
	3
	

	Square billet
	50-65
	+/-1,5
	10
	6
	
	3
	

	
	70-90
	+/-2,0
	10
	6
	
	3
	

	
	100-120
	+/-2,5
	10
	6
	
	3
	

	
	140
	+/-3,0
	10
	8
	
	3
	

	
	160
	+/-4,0
	10
	8
	
	3
	

	Round bar

with peeling
	14-190
	DIN EN 10060

h11-h13
	DIN EN 10060
	< 5
	DIN EN 10060
	
	

	Round bar

without peeling
	15-150
	DIN EN 10060


	DIN EN 10060
	< 5
	DIN EN 10060
	
	

	Round bar with special surface finishing
	2-120
	h10-h13

To be agreed
	0,5-1,0
	
	Not more than

50 % of max tolerances sum
	
	


Note: according to agreement the bars with special surface finishing, dia. 2-120mm  should be delivered with max tolerances j (tolerances +/-) and k (tolerance +).

Other delivery terms:

· It is possible to produce steel material according to the Customer`s special technical requirements with preparing of necessary technical documentation;

· The steel products should be delivered in accordance with standards: EN, ISOM DIN, UNI, AFNOR, INTERNATIONAL (HAYNES/HAYNES), ASTM, AISI, JIS OR OTHER/
3. SURFACE QUALITY OF STEEL PRODUCTS

	Surface defects

	Kind of products
	Non permissible
	permissible

	Bloom (170 – 250 mm)

Square billet 

(50 – 160 mm) 

without surface conditioning
	Rolling skin, laps, cracks
	isolated fine marks, roll marks, pitted surface, hair lines with the depth 8% max from nominal size 

	Square steel billet (50 – 160 мм), suitable for forging/hot forming 
	Scab, cracks, roll marks
	Pitted surface, expanded blisters, dirty spots of the depth max 0,4mm

	Peeled bars

(14 – 190 mm)
	
	Mechanical defects, the depth should not exceed the tolerance for the nominal diameter 

	Bars without peeling

(15 – 150 mm)
	Scab, roll marks, cracks, dirty spots
	Isolated fine marks, dents, pitted surface, the depth should not exceed ½ sum of max. tolerances

	Bars with special surface finishing 

(2 – 120 mm)
	
	Mechanical  defects of the depth ½ of the tolerance for nominal diameter


Note: surface quality of round bars meet the requirements of  EN 10221 «В» or «С» class (the class of surface quality is specified during the registration of an inquiry).
