	Dutch Wire Mesh

Materials: stainless steel wire ,low carbon steel wire .
Weaving: plain weave, twill weave, bamboo-type weave, twist weave.
Character: It is fine and have the stably performance.
Uses: used in spaceflight, oil, chemical industry etc. 


[image: image1.jpg]



 

 

Mesh 

Wire Dia. (MM)

Material (AISI)

12mesh x 64mesh

0.58 x 0.40

304 or 316

24mesh x 110mesh

0.36 x 0.25

304 or 316

14mesh x 88mesh

0.50 x 0.33

304 or 316

30mesh x 150mesh

0.23 x 0.18

304 or 316

40mesh x 200mesh

0.18 x 0.13

304 or 316

50mesh x 250mesh

0.14 x 0.11

304 or 316

80mesh x 700mesh

0.10 x 0.08

304 or 316

165mesh x 800mesh

0.071 x 0.040

304 or 316

165mesh x 1400mesh

0.06 x 0.04

304 or 316

200mesh x 1800mesh

0.05 x 0.032

304 or 316

825mesh x 2300mesh

0.035 x 0.025

316L

400mesh x 2800mesh

0.030 x 0.02

316L


	


