Expanded Metal Mesh

Materials : aluminium plate ,thin low carbon steel plate, stainless steel plate, Al-Mg alloy plate, copper plate, nickel plate. 
Weaving and characteristic: It is punched to mesh, including aluminum plate mesh, small steel plate mesh, steel plate mesh and stainless steel plate mesh ;according to the hole, it is divided to diamond, square, round, triangle, scale hole. it is strong and wear resisting, artistic and tasteful. 
Uses: used wide in road, railway, civil building, water conserrancy's building; the protecting of all kinds of machines. Electrical equipment, window and aquatic product's breed. 

	
	[image: image1.jpg]




	Specification of Expanded Metal Mesh

Sheet Thickness

Opening in Width
mm

Opening in Length
mm

Stem

Roll Width
mm

Roll Length
mm

Weight
kg/m2
0.5

2.5

4.5

0.5

0.5

1

1.8

0.5

10

25

0.5

0.6

2

0.73

0.6

10

25

1

0.6

2

1

0.8

10

25

1

0.6

2

1.25

1

10

25

1.1

0.6

2

1.77

1

15

40

1.5

2

4

1.85

1.2

10

25

1.1

2

4

2.21

1.2

15

40

1.5

2

4

2.3

1.5

15

40

1.5

1.8

4

2.77

1.5

23

60

2.6

2

3.6

2.77

2

18

50

2.1

2

4

3.69

2

22

60

2.6

2

4

3.69

3

40

80

3.8

2

4

5.00

4

50

100

4

2

2

11.15

4.5

50

100

5

2

2.7

11.15

5

50

100

5

1.4

2.6

12.39

6

50

100

6

2

2.5

17.35

8

50

100

8

2




