Prepainted Coils

Specifications & Information

Base Material
:
Galvanized Coils and/or CRM coils

Type of Prepainted Products
:
1. Color Product

2. Laminated Product

3. Emboss Product

Type of Finish Coat
:
Polyester  (1-Normal, 2-with  ‘HD’ and/or with ‘DHD’

3-Polyurtan, 4-PVDF, 5-PVC

Type of Stripable Film
:
With or without film

Number of Color
:
RAL 9001/10/16, RAL 5012/15 and 

RAL 3000/3020/6024/6029

Finish Coat Thickness
:
Coat thickness between 10 to 200( for Plastisol, Top Coat thickness is 100-200(

Type of paint on bottom surface
:
Polyester

Zinc Coating mass
:
200/220/250 and  275gr/m2  JIS 3302   

Steel grade
:
CGCC (according to JIS G 3312/94)

Dimensional Limits
:
Thickness : 0.5 – 1.2 mm

Width       : 750 – 1250 mm

End Uses
:
Direct (1-Building in Humidity Condition, 2-Building in Sea Side, 3- building in Normal Condition, 4 – panel

Dimensional Shape & Camber Tolerance
:
JIS G 3312

Technical Tests
:
Per Cast/Per Item/Per Cast-item and per rolled unit

Quality Certificate
:
According to DIN 50049 3.1.B / Mill Test report/Mill Test Certificate and Inspection Certificate

Inside Diameter
:
508mm and/or 610 mm

Outside Diameter
:
915mm MIN – 1900 MAX

Coal Weight
:
1000mm Width = 4.7-8.4MT, 1100mm Width = 5.1 – 9.2 MT , 1200mm-1290mm width = 5.5 – 10 MT

Packing 


:
Code 807 – Tarred Paper wrapping steel flanged crown for protection of Coil Crown -steel sheet for outside

Protection - Serrated Collars for Outside Edge – inside collars bound with 3 circumferential and 5 radial straps. 

Code 808 – Tarred Paper wrapping steel flanged crown for protection of Coil Crown -steel sheet for outside

Protection - Serrated Collars for Outside Edge – inside collars bound with 3 circumferential and 5 radial straps. 

Wooden Pallet fastened with 3 radial strap.

