	MUBARAKIA
	Mubarakia Marine Services Co.

[image: image1]

	MARINE
	


Construction of New Berth at Umm-Qasr Port, Iraq
	MUBARAKIA

	MARINE



Specifications for Tubular Piles
	No
	Description of Tubular Steel Bearing Piles
	Meters

	1
	Pile 711mm diameter x 12.7mm thick
(28" x 0.562")
	2,664

	2
	Pile 864mm diameter x 12.7mm thick
(34" x 0.562")
	5,472

	3
	Pile 914mm diameter x 16.0mm thick
(36" x 0.688")
	2,088

	4
	Pile 965mm diameter x 16.0mm thick
(38" x 0.688")
	3,312


Specifications:

1. Spirally Welded Steel Pipes (SAW)

2. Grade 50 steel, to BS-4360 or equivalent
3. Length shall be 12 meters long, beveled from both ends
4. Preferred length is 30 meters
Coating Details:

· Surface preparation, blast clean first quality

· 1st coat with 2 pack epoxy zinc phosphate blast primer

· 2nd coat with 2 pack epoxy under coat

· 3rd coat with 2 pack epoxy finish

· The minimum total dry film thickness shall be 200µ m
PO Box 9460, Ahmadi 61005, Kuwait    www.mubarakia.com
( 398-4984  Fax:(+965) 398-3311   ( e-mail: mks@mubarakia.com

[image: image1]