[image: image1.png]


                                                                         Belitskaya Enterprise

External economic  agency

640000,Russia,Kurgan,Uritskogo  str.28    

‏‏Tel:+73 52 245-9277

Fax:  |+73 52 245-9277

                                                                                            Mobile:+7 9128329204/+79128312171
                                                                                                                   Email: sld@r45.ru:

Fabricant: JSC  NOSTA , ORSK-KHALILOVO  IRON AND  STEEL  WORKS 

HOT  ROLLED  STEEL  SQUARE BILLETS 

As usual  steel  billets  are manufactured  according  to GOST  380-94,

 TU  14-1-5237  or   TU 14-1-44920 

 Steel Grades options: 3SP/PS, 5SP/PS, ASTM  A36/A 572  

	Cross-section  sizes,mm
	Side  tolerances,mm
	Maximum  corner  

radius   , mm

	90x90
	+/- 2.0
	12

	100x100
	+/- 2.4
	15

	120x120
	+/- 2.7
	18

	125x125
	+/- 2.7
	18

	130x130
	+/- 3.2
	21

	140x140
	+/- 3.2 
	21

	150x150
	+/- 3.2
	21

	160x160
	+/- 3.9
	25

	180x180
	+/- 3.9
	25

	200x200
	+\- 4.5
	30


Straightness  deviation: maximum  12 mm  per  meter  

	Cross-section sizes


	Length,mm



	100х100


	5950,6350,6800, 7300, 7950, 8650, 9550, 10600, 11950



	120х120


	5900, 6500,7250, 8150, 9300, 10850



	125х125


	6000, 6650, 7500, 8550,10000



	130х130
	5550, 6150, 6950 

	140х140
	5950,6800,7950, 9550, 11950

	150х150
	5900, 6900, 8300, 10350

	160х160
	6050, 7300, 9150

	180х180
	5700, 7150, 9550

	200х200
	5750, 7700, 11550


Order of  length 5800-11800  mm can  be placed  in  production  programm,  however 10-15%  of  unmeasured  length shall  be  supplied  as agreed  with  customer.  

	Pig iron

	elements, %

micro elements, %

Si

Mn

S

P

C

Cu

V

Ti

Cr

0,5-1,2

0,1 max 1,0 max

0,03 max

0,10 max

3,5-4,5

0,02 max

0,01 max

0,015 max

0,03 max

elements, %

micro elements, %

Si

Mn

S

P

C

Ti

Cr

Cu

V

Pb

0,10-0,50

0,05-0,10

0,015 max

0,050 max

3,5-4,5

0,010-0,030

0,005-0,040

0,005-0,020

0,010-0,030

-

Pb, Al, Co, Sb, B, Te, As, Sn, Mo, 
Se, Zn, Bi, Ni  0,030 

0,5-1,0
1,0-1,5
1,5-2,0
2,0-2,5

0,10 max

0,020 max

0,06 max

3,5-4,5

0,025 max

0,01 max

0,01 max

0,01 max

0,01 max

Al, Co, Sb, B, Te, As, Sn, Mo, 
Se, Zn, Bi, Ni  0,030 

Grade

elements, %

micro elements, %

Si

Mn

S

P

C

Cu

V

Ti

Cr

L1
L2
L3
L4
L5
L6 

3,21-3,60
2,81-3,20
2,41-2,80
2,01-2,40
1,61-2,00
1,21-1,60

0,5-1,0

0,03 max

0,10 max

3,5-4,5

0,03 max

0,01 max

0,04 max

0,06 max

Weight of ingots - 10 kg
Any grade of pig iron can be produced according to the customers' requirements 


Savings Bank  of the  Russian  Federation (Uralsky  office) Kurgan Branch 8599  SWIFT: SABRRUMMEA1, acct.no. 408.028.404.320.201.007.62, The Bank  of New York, acct.no. 890.0057.610,SWIFT:IRVTUS3N , Trade reg. no 35832.,  VAT No.450102605174  


