[image: image1.png]


                                             Belitskaya Enterprise

External Economic agency

640000,Russia,Kurgan,Uritskogo  str.28    

‏‏Tel/Fax:0073 52 245-9277

Mobiles: 007912-8329204/8312171

                                                                                                                                        sld@r45.ruEmail:

              All about Russian scrap ( all grades)           

The scrap is classified according to St. Standard GOST 2787-75.

The price depends on the quality of the scrap, its quantity and regularity of the deliveries. The price may also change depending on the variation of prices for the raw material on the world market (London Metal Exchange) and the Ruble-USD rate. 

Types of scrap           Composition                               Size and weight 

1A                              Lump scrap            Size up to 300x200x150 mm, thickness from 

                                                                  6 mm, weight from 0.5 to 40 kg. 

2A                              Lump scrap            Size up to 600x350x250 mm, thickness from

                                                                  8 mm, weight from 2 kg.  

3A                              Lump scrap            Size up to 800x500x500 mm, thickness from

                                                                  6 mm. Channels and I-beams with a wall 

                                                                  thickness up to 4 mm are allowed in a 

                                                                  quantity of 20% 

3A1                            Lump  scrap          Size   up  to 1500x500x500mm, thickness

                                                                   from 6 mm  ( equivalent to HMS )      

4A                              Lump scrap 

                                   (metalware)            Size up to 200x150x100 mm, thickness from 

                                                                   6 mm, weight from 0.025 to 20 kg.  

5A                             Oversize scrap         Thickness from 6 mm.  

8A                     Bales of sheet, strip, pipes.

                                 Chip is allowed        Size up to 2000x1050x750, density from

                                                                  2000 kg/m3, weight from 40 kg. 

9A                          High-density bales. 

                                      No chip.               Size up to 2000x1050x750, density from

                                                                   1800 kg/m3, weight from 40 kg.  

10A                        High-density bales. 

                               Chip is allowed           Size up to 2000x1050x750, density from

                                                                   1200 kg/m3, weight from 40 kg.  

11A                        Sheet, strip, waste,

                                   pipes, roofing, 

                              light-weight scrap        Linear size up to 3500x2500x1000 mm,

                                                                   thickness up to 6 mm.  

12A                        Sheet, strip, waste, 

                pipes, roofing, light-weight 

                                  scrap, wire               Linear size up to 3500x2500x1000 mm,

                                                                   thickness up to 6 mm.  

13A                  Steel rope and wire           Bundle dia. up to 1000 mm, length up to 

                                                                   500 mm, weight from 20 kg 

14A           Discontinuous chip and 

                  scissel. Lumps, no balls           Coil length up to 50 mm. Coils up to 100 

                                                                    mm are allowed in a quantity of 3% of the 

                                                                     weight. Scissel up to 0.025 kg.  

15A         Chip and scissel. No lumps          Coil length up to 100 mm. Coils up to 200

                                                                      mm are allowed in a quantity of 3% of the 

                                                                      weight. Scissel up to 0.05 kg.  

16A          Curled chip. No lumps                Not regulated 

17A     Lumps of machine iron castings,

            secondary cast iron pigs                   Lump size up to 300 mm, weight from 0.5

                                                                      to 20 kg. Lumps with a weight up to 0.5 

                                                                      kg are allowed in a quantity of 2%.  

18A     Lumps of cast iron moulds 

                  and mould plates                         Lump size up to 300 mm, weight from 0.5

                                                                       to 40 kg. Lumps with a weight up to 0.5 

                                                                       kg are allowed in a quantity of 2%.  

19A    Lumps of iron castings with 

            a high phosphorus content. 

Lumps of malleable cast iron and pipes       Lump size up to 300 mm, weight from 0.5

                                                                      to 20 kg. Lumps with a weight up to 0.5

                                                                      kg are allowed in a quantity of 2%.  

20A Lumps of machine iron castings           Not regulated 

21A Lumps of cast iron moulds and 

                  mould plates                                Not regulated 

22A Lumps of iron castings with a 

            phosphorus content. 

Lumps of malleable cast iron and pipes       Not regulated 

24A        Cast iron chip                                 Not regulated 

Our company sells ferrous scrap. The products offered for sale are cleaned from impurities, sorted out by types and sizes in accordance with St. Standard GOST 2787-75

                         Shredding of aluminum and steel scrap.

Shredding is carried out on a HKS-1250-23-III-U Thyssen shredder with a capacity of 35 to 50 t/hr. The initial material is loaded on an apron feed conveyer and is directed to the shredder via a slanting stationary chute. The material ground in the shredder is fed to a blow-through chamber where volatile materials and light impurities are separated from metal scrap. Then the cleaned metal scrap is passed through a magnetic drum where the magnetic metal fraction is separated from the non-magnetic fraction. Operation of the shredder is based on the straight passage of the material through all processing stages, which avoids congestion and undesirable accumulation of scrap. Such process makes it possible to obtain a high-quality raw material with a density of 1.0 to 1.5 t/m3 from dirty metal waste. This material is supplied to metallurgical plants. 

2. Separation of the magnetic fraction from the non-magnetic fraction (Al, Ni, Cu, Zn, etc.).

The shredder makes it possible to separate up to 90% of the magnetic or non-magnetic fraction, depending on the raw material. 

3. Processing of aluminum waste, such as lumps, chips and slag.

Aluminum lump scrap is processed as follows:

The scrap delivered to the enterprise through a radiation control system is weighed, sorted out into groups and fed to the processing plant in accordance with the heat log. The finished products are weighed and brought to the warehouse. 

The chip delivered to the enterprise through a radiation control system is weighed, crushed, dried, separated and fed to the processing plant for remelting. 

The aluminum slag delivered to the enterprise through a radiation control system is weighed and fed to the slag enrichment plant manufactured by US firm Altec and Spanish firm Remetal. The concentrate obtained as a result of enrichment is separated and fed to short-drum furnaces for melting. The finished product is weighed, bundled, marked and brought to the warehouse. 

4. Disposal (burial) of aluminum waste (slag with low aluminum content).

Our company can arrange for disposal of aluminum slag with low content of metal aluminum. The disposal cost is fixed in each concrete case. The company has its own disposal facilities dully fitted out in accordance an Austrian technology and approved by the competent authorities of the Russian Federation. Metal furnace sludge is accepted for disposal by our company free of charge; in some cases we can pay for the sludge if its metal content is larger than 60% of its gross weight. 

6. Cropping of large-sized ferrous scrap at the storage site.

For enterprises which, due to objective reasons, cannot carry out cropping of large-sized scrap we have formed mobile teams which carry out scrap cropping at the client's storage site. 

Savings Bank  of the  Russian  Federation (Uralsky  office) Kurgan Branch 8599  SWIFT: SABRRUMMEA1, acct.no. 408.028.404.320.201.007.62, The Bank  of New York, acct.no. 890.0057.610,SWIFT:IRVTUS3N , Trade reg. no 35832.,  VAT No.450102605174  


